## Slide 1: MMIC Design Flow
Anurag Nigam

## Slide 2: Tutorial 2
Day1
Bias Decoupling or Matching
Bias Decoupling or Matching
Output Matching
Input Matching
Active Device
1
2
3

## Slide 3: Six Caps of a MMIC Designer
Circuit Design
Layout & EM Simulations
Package Design & EM Simulations
Thermal Design & Modeling
Sensitivity, Yield & DOE
Board Designs & Assembly
RF Testing
Design Spins
& Documentation
MMIC stands for ‘Monolithic Microwave Integrated Circuit’. Due to high frequency, dimensions of lumped components are comparable to wavelength. This makes lumped components behave like distributed circuits. Substrate coupling, package & board parasitic dominate and affect the response of MMIC.

## Slide 4: On Chip MMIC Circuits
Digital Attenuator
Digital Phase Shifter
Power Amplifier (PA)
Low Noise Amplifier (LNA)
T/R Switch (SPDT)
Circulator
Patch Antenna Array
Patch Antenna
Power Limiter
Voltage Controlled Oscillator (VCO)
Mixer
Band Pass Filter (BPF)
High Pass Filter (HPF)
Low Pass Filter (LPF)
Band Stop Filter (BSF)
Power Combiner/ Divider
Hybrid

## Slide 5: Typical Gain Block
Bypass Cap
At DC, Bypass Capacitors are open. At RF, ideally, Bypass Capacitors are short . Role of this capacitor is to isolate Device Impedance from output impedance of DC Supply Voltage.
Coupling Cap
Role of Coupling Capacitor is to couple Device and Source/Load Impedance at RF and isolate DC from Load and Source Impedance. This capacitor can be small and part of high pass matching circuit.
Bias Decoupling or Matching
Bias De-coupling circuit impedance appears in parallel to device impedances. Ideally they should be open circuit at frequency of interest so as to provide full Smith Chart Impedance Range. Th demerit is narrow band width of the circuit and stability issues at high frequency.
Instead of Bias Decoupling, an inductor can be used as part of matching. The merit of using low value inductor is low DC drop across it resulting is higher -1dB Gain Compression Point of Circuit and better stability at High Frequency. Demerit of using an Inductor is lower Impedance Range (Excursion to edge of Smith Chart is not possible, not suitable for large transistors with small impedances)
Device Impedance
Device Impedance
With inductive load
Input/output Matching
Matches Device Impedance to 50Ω. Lossless network is bilateral
Bias Decoupling or Matching
Bias Decoupling or Matching
Output Matching
Input Matching
Active Device
Active Device
Active device provides RF Gain.

## Slide 6: Typical Absorptive Type Switch
1
2
3
Bypass Cap
Coupling Cap
Roles of Coupling Capacitor & Bypass Capacitor are explained earlier.
Bias Decoupling
Resistance is used for decoupling as the gate does not draw any current. Bypass Capacitor and decoupling resistance present impedance to gate that decides phase of S21 across the pass transistors T1 and T3.
Pass Transistors
When On, Pass Transistors decide Insertion Loss of the switch. Insertion loss of switch in On path decides Power Capability of Transmit Chain and Noise Figure of Receive Chain.
When Off, Drain to Source Capacitance of Pass Transistors decides Off Path Isolation.
Bypass Transistors
When On, Bypass Transistors terminate the off port in 50Ω.
When Off, Drain to Source Capacitance of Bypass Transistors decides on port impedance and hence the insertion loss of On Path.
Operation in brief
For Port 1 to be connected to Port 2, T1 and T2 are On and T3 and T4 are Off.

## Slide 7: Gallium Arsenide (GaAs) Process
4” GaAs Wafer
1 GHz
2 GHz
5 GHz
10 GHz
20 GHz
50 GHz
100 GHz
HP 07 Power MESFET (0.7um)
PPH 25 Power PHEMT (0.25um)
PPH 25x High Power PHEMT (0.25um)
PPH 15 Power PHEMT (0.15um)
PH 25 Low Noise PHEMT (0.25um)
PH 15 Very Low Noise PHEMT (0.15um)
HB20P R/O High Power /Oscillator InGaP HBT
HB20L Low Cost InGaP HBT
HB20S Very High Power
L-S Band InGaP HBT
BES 100 Schottky Diode Technology
Various UMS GaAs Processes
Process we will explore through our designs

## Slide 8: UMS PH 15 Process Summary

## Slide 9: Layout Design Rules
Cell Names should not conflict
Only capital are acceptable in cell names
Maximum of 16 characters are acceptable in cell names
‘A’-’Z’, ‘0’-’9’ and ‘_’ are only acceptable characters in cell names
Maximum vertices acceptable in a polygon is 200
All polygons should have enclosed areas. Lines, poly-lines and curves are not acceptable
Hierarchical Layout is acceptable (No need to flatten p-cells)
At Wafer Level all dimensions should be multiples of 1um
Coincident patterns and cells including GR and PL Layers are not acceptable
Transistor Gate Widths should be along horizontal direction
Angles should be multiple of 45° or 90° except for patterns in EL Layers
Chip dimensions should be multiple of 10 um
Chip aspect ratio should be less than 3
Minimum distance between any pattern and dicing street is 20 um
Minimum distance between Substrate Via edge and dicing street is 55 um
Minimum dimensions of bond pad are 100 um x 100 um
Minimum distance between bond pads is 50 um
Text is written in CO Layer using DRC free UMS Alphabets
Dicing streets should be continuous across the wafer
6 mm x 6.1 mm < tile size< 14 mm x 14 mm
Substrate Via in straight lines are not acceptable
Tile y dimension should not be in range 7 to 7.45 mm, 9 to 9.58 mm, 12.6 to 13.4 mm
Area has to be reserved for PCM Cell
Minimum distance between bond pad and air bridge is 50 um
Minimum distance between MIM Capacitor and bond pad is 50 um

## Slide 10: UMS PH 15 Process- Substrate Via
First Step in design at microwave frequency is to determine Substrate Via Inductance
First Effort to setup EM Simulation is ADS is to define Metal Stack
We have to inspect other components to have complete idea of Substrate Definition in ADS
EL
DPC
TR
EL
DPC
TR
N1
CO
GaAs
CO
30 x 30
80 x 80

## Slide 11: MIM Capacitor
air-bridge (PEL)
DPC
EL
N1
Dimensions of top electrode
Dimensions of bottom electrode
Dimensions of the bridge

## Slide 12: Air Bridge
EL
PEL
Silicon Nitride Passivation
With Boron Implant
Gold Plated Metal (EL)
Air
TiPtAu Metal (N1)
Silicon Nitride (MIM)
GaAs
Gold Plated Metal (TR)

## Slide 13: Approximate Substrate Definition in ADS
PEL
Bridge
EL
N1
GaAs
Cond
MIM_SiN
Pass_SiN
Model: Thick (up), thickness: 3.3um, Real: 5.8e7S/m
Model: Thick (down), thickness: 2.69mil, Real: 4.1e7S/m
EL_VAB
DPC
EL_DUMMY
Model: 2D Distributed, Real: 3.4e7S/m
DPC_VIA, DPC
Model: Thick (up), thickness: 3.3um, Real: 5.8e7S/m
Model: Thick (up), thickness: 0.5um, Real: 3.4e7S/m
FreeSpace
FreeSpace2
Boundary: Open, Er -Real: 1, Loss Tangent: 0
Boundary: Open, Er -Real: 1, Loss Tangent: 0
Thickness: 100 um, Er -Real: 12.8, Loss Tangent: 0.0003
T: 0.19 um, Er -Real: 7.2, TanD: 0.0004
T: 0.2 um, Er -Real: 7.2, TanD: 0.0004
Thickness: 2 um, Er -Real: 1, Loss Tangent: 0
DPC_VIA
CO
Model: Thick (up), thickness: 0.19um, Real: 0.125e7S/m
EL_VAB
Model: 3D Distributed, Real: 3.4e7S/m
Model: 3D Distributed, Real: 4.1e7S/m
EL_DUMMY

## Slide 14: Microstrip Lines
EL
GaAs
Cond
T
W
L

## Slide 15: TaN Resistance

## Slide 16: TiWSi Resistance

## Slide 17: GaAs Resistance- SiN with Boron

## Slide 18: Inductors
Fixed inner radius n=20 um
air-bridges
Input node
Output node
Fixed 26 um x 26 um
Fixed Spacing s=5um
Variable Width
W=5, 10, 15, 20 um
EL
N1

## Slide 19: Maximum Current Ratings
Layer | Component | Max. DC current | Max. RF Power | Imax1(Mean) | Imax2(RMS)
EL | Line, inductor, bridge | 7.5 mA/ um |  | 7.5 mA/ um | 47 mA/ um
GR/PL | FET gate | - |  | 3 mA/ um | 3mA/ um
RM | TaN resistor | 0.4 mA/ um | 5 uW/ um sqr. | 0.45 mA/ um | 1 mA/ um
RHRW | TiWSi resistor | 0.1 mA/ um | 10 uW/ um sqr. | 0.4 mA/ um | 0.2 mA/ um
N1 | Inductor, interconnection | 2 mA/ um |  | 2 mA/ um | 22 mA/ um
ZAL | GaAs resistor | 0.8 ma/ um | 77 uW/ um sqr. | 0.8 mA/ um | 0.8 mA/ um

## Slide 20: Dicing Street Rules

## Slide 21: PHEMT Device Models
GaAs
InGaAs
AlGaAs
Ohmic metal (CO)
T-shaped Al Gate
Silicon Nitride Passivation
TiPtAu (N1 Metal)
Silicon Nitride Dielectric
Gold Plated Metal (EL)
Linear Model for Low Noise Amplifier Design
Non-Linear Cold Model for Switching Circuits
Non-Linear Hot Model for Power Circuits

## Slide 22: Maximum DC Ratings

## Slide 23: Layout Guidelines
Layer Name | GDSII Num. | Technological process step | Min. Grid
ZAL | 02 | Boron Isolation | 0.1 um
CO | 03 | Ohmic Contacts | 0.1 um
PL | 41 | Gate Bus | 0.005 um
GR1 | 14 | Gate (0.15 um) | 0.005 um
GR2 | 44 | Gate (other dimension) | 0.005 um
OUV | 38 | Nitride Opening on CO | 0.1 um
RHRW | 16 | TiWSi resistor | 0.1 um
RM | 06 | TaN resistor | 0.1 um
RMG | 17 | Al/ Au diffusion barrier layer | 0.1 um
N1 | 04 | MIM bottom electrode | 0.1 um
DPC | 05 | Nitride Opening | 0.1 um
PEL | 39 | Air-bridge Layer | 0.1 um
EL | 40 | Gold Plating Metal | 0.1 um
TR | 10 | Via-hole | 0.1 um
DCFA | 11 | Backside Dicing Street | 0.1 um
The recommended grid size for layout is 1 um. Sub-micron grid is acceptable in cells. Spacing, Width, Overlapping, Overhanging, and Enclosure rules for various layers should be read prior to attempting layout and layout based designs